# TECHNICAL DESCRIPTION SHEATHING CONSTRUCTION

| Special Pose No. | 1 PLASTERING |  |  |
| --- | --- | --- | --- |
| Definition | Plastering with 250/350 kg cement dose coarse and fine mortar (exterior plaster) |  |  |
| Long Definition | PLASTERING WITH 250/350 KG CEMENT DOSE COARSE AND FINE MORTAR (EXTERIOR PLASTER) |  |  |
| Unit | M2 |  |  |
| Pose Description, Construction Conditions and Measurement |  |  |
| Rough plastering with an average thickness of 2 cm with mortar prepared by adding 250 kg cement to 1 m3 toothed sand, thin plastering with an average thickness of 0.8 cm with mortar prepared by adding 350 kg cement to 1 m3 spindle sand, cleaning the wall surface, watering when necessary, all kinds of materials and wastage, labor, work tables, loading at the construction site, horizontal and vertical transportation, unloading, including contractor's overhead and profit, 1 m2 price: MEASURE : All plastered surfaces are calculated over the project. |  |  |

| Special Pose No. | 2 SHEATHING CONSTRUCTION |
| --- | --- |
| Definition | 4 cm thick rock wool boards (min. 120 kg / m3 density) with external thermal insulation on exterior walls and thermal insulation plaster on it (sheathing) |
| Long Definition | 4 CM THICK ROCK WOOL BOARDS (MIN. 120 KG / M3 DENSITY) WITH EXTERNAL THERMAL INSULATION AND THERMAL INSULATION PLASTER ON THE OUTER WALLS (SHEATHING) |
| Unit | M2 |

## Pos Description, Construction Conditions and Measurement

According to the project and details, on the exterior walls, 4 cm thick, rock wool boards are adhered to the wall with thermal insulation board adhesive with a consumption of 4 kg per m², then fixed to the surface with steel studded thermal insulation dowel, and 1. layer of thermal insulation plaster, placing the plaster net on it so that the joints overlap each other by at least 10 cm and plastering the 2nd layer of thermal insulation plaster on it with a consumption of 2 kg per m², loading, horizontal and vertical transportation, unloading, all kinds of materials and losses, labor, tools and equipment expenses, contractor's general expenses and profit, including 1 m² price: MEASURE: All insulated surfaces are calculated according to the dimensions in the project. NOTE:1) The thickness of the rock wool board will be determined according to the heat calculation. 2) The dowel to be used will be determined according to the material properties

on the facade to be sheathed. 3) Exterior thermal insulation systems must comply with the criteria specified in TS EN 13500 system standard or ETAG 004.

# TECHNICAL SPECIFICATION

### NOTE: THERMAL INSULATION BOARD, ADHESIVE, PLASTER AND PAINTS TO BE USED IN THE THERMAL INSULATION PACKAGE SYSTEM WILL BE BRANDS WITH TSE CERTIFICATE.

SPECIAL 1 :Rock wool Board 4cm 120 kg/m3 Density

# INSULATION BOARD

4 cm thick rockwool boards (rockwool - 120 kg/m3 density-loadable) with horizontal thermal insulation (traditional walkable terrace roof, etc.)

-Thickness: 4 cm thick rock wool boards will be used.

-Corners should be mitered and angular deviations should not exceed +- 2 mm per meter.

# TECHNICAL SPECIFICATIONS

It is formed by melting basalt stone, which is an inorganic raw material, at 1350°C-1400°C and turning it into fiber.

It can be produced in different sizes and technical specifications, with different coating materials, in the form of mattresses, sheets, pipes and casts, depending on the place and purpose of use.

In building exterior sheathing,

It is used for thermal insulation, sound insulation, acoustic regulation and fire insulation. Thermal conductivity declaration value is ?? 0,037 W/mK.

The water vapor diffusion resistance factor µ=1. Operating temperature in the range -50/+600, -50/+650°C.

Even when exposed to heat and humidity, there should be no change in its dimensions.

It should not deteriorate over time, rot, mold, corrode or rust. It must be indestructible by insects and microorganisms.

According to TS EN 13501-1, "non-combustible materials" should be in A1 class.

Izocam Rockwool products subject to TS 901-1 EN 13162 Standard must bear CE marking within the framework of Construction Products Directive (89/106/EEC).

# MATERIALS USED IN THE APPLICATION

### INSULATION BOARD

4 cm thick rockwool boards (rockwool - 120 kg/m3 density-loadable) with horizontal thermal insulation (traditional walkable terrace roof, etc.)

-Thickness: 4 cm thick rock wool boards will be used.

-Corners should be mitered and angular deviations should not exceed +- 2 mm per meter. 1.2)ADHESIVE

It must be manufactured from portlantd cement and acrylic and resin dispersion powder according to TS, ISO certified DIN 1164. Tensile strength should be >0,1 N/mm2 on polystyrene and less than 1,0 N/mm2 on concrete.

### PLASTER FILM

It should be woven from glass fiber that provides hardness and strength by spreading the impacts on the surface that meets the tensions that may occur on the plaster surface, prevents cracks, provides hardness and strength by spreading the impacts on the surface, with a pore range ranging from 3.5-5 mm and impregnated with a binder that will not dissolve in alkaline environment. Density should not be less than 160 g/m2.

### PLASTIC ANCHOR

It is a 10 mm diameter, 150 mm wide head dowel with polyethylene body made of hard plastic, polyamide nail, recycled plastic-free, 10 mm diameter, 150 mm size steel nail for anchoring insulation boards to the facade surface.

### CORNER REINFORCEMENT PROFILE

It is a perforated aluminum profile with 0.6 mm wall thickness and 25/25 mm sized surfaces, which should be used in external corners such as building corners and window centers to protect the system and act as a gauge in plaster application.

### PLASTER MATERIALS

TSE, ISO or DIN certified plaster material with elastic additives consisting of cement-acrylic mixture with special granulometer (max. 1 mm) inorganic fillers and additives, Min compressive strength 15 N/mm2 (for 3 mm thickness) diffusion value 0,02 meter; flexural strength 7,5 N/mm2 Shrinkage 0,8 mm/m.

### DECORATIVE PLASTER

Must be TSE, ISO or DIN certified. It is a mixture of inorganic filler and acrylic with cement special granulometer (max. 2 mm grain diameter), breathable, waterproof, impact resistant,

white colored, flexible topcoat material. Diffusion value 0.06 meter -1, capillary water absorption value 0.10 kg/m2h ½

### TOPCOAT PAINT

Silicone-added acrylic-based breathable exterior paint that can be applied with a roller with high coating feature will be used.

# APPLICATION

### SURFACE PREPARATION

Surfaces are checked before starting the exterior thermal insulation system. Defects exceeding 1 cm vertically and horizontally are corrected with rough plaster. Dust and foreign material on the surface are cleaned.

### BONDING OF INSULATION BOARDS

After the application surface is made suitable, the special adhesive with the properties specified in article 1.2 is mixed with water and brought to a paste consistency and applied to the insulation boards with a consumption of 5 kg per m2 and after combing or evenly distributed per board and applied in a heap to a minimum of 12 points, vertical joints are staggered on the plumb line and horizontal installation is made from bottom to top.

During the gluing process, the surface should be checked frequently with a gauge and spirit level. If there is a level difference between the boards, the protrusions should be filed. The contact surfaces of the boards with each other should be tight and continuous, and there should be no adhesive between them (to prevent the formation of a thermal bridge).The boards should not be left open to weather conditions for a long time and should not be exposed to ultraviolet rays.

### BONDING OF INSULATION BOARDS

Doweling should be done at least 24 hours after the bonding process. Dowels with the specifications in article 1.4 should be applied to the corners and center of each plate, approximately 5 per m2.

### CORNER PROFILE ASSEMBLY

Since the corner profiles will also act as a gauge for the plaster to be applied at the same time, after the insulation boards are adhered, the corner profiles with the properties specified in item

1.5 are adhered with elastic bottom layer plaster (item 1.6) before the plastering stage. It is applied on all window centers and building corners.

### APPLICATION OF PLASTER AND PLASTER FILM

The insulation boards are cleaned by wiping with a damp cloth, the plaster material containing the properties in article 1.6 is mixed with water and brought to a paste consistency and applied to the surface with a trowel. While the plaster is still fresh, the plaster mesh containing the properties in article 1.3 is brought to the surface and it is ensured to be embedded into the plaster with the help of a roller or spatula. Mesh joints min. 10 cm overlapping each other. An additional layer of mesh is applied on the window corners and left to dry. After the surface dries, the 2nd layer of plaster is applied in the same way and the plastering process is completed.

### TOP COAT DECORATIVE PLASTER APPLICATION

After the plastering stage, the decorative plaster is applied to the surface with a steel trowel. Before it dries, it is troweled in circles with a plastic trowel. Application min. 2 mm. thickness and consumption should not be less than 2.5 kg/m2. Areas connected to each other are plastered as a whole without leaving any gaps.

### TOP COAT PAINT

1.7 The paint material containing the properties in article 1.7 is applied in two coats with a roller brush after the top coat of decorative plaster is applied and dried. The first coat of paint should be applied by diluting 10% and the second coat should be applied undiluted with a total consumption of 0.3-0.4 kg / m2.

## Special POS 3: SCAFFING SUPPLY

SPECIAL 2: Scaffolding supply, installation and dismantling workmanship, all kinds of materials and losses, loading, horizontal and vertical transportation, unloading, labor, tools and equipment costs, contractor's profit and overhead costs included 1m2 price: MEASURE : Scaffolding is calculated in "m2".

## Special POS 4: PAINTING

| Pose No |  |
| --- | --- |
| Definition | Acrylic based water-based paint on exposed concrete, plastered or old painted surfaces after applying primer (exterior) |
| Long Definition | Acrylic based water-based paint on exposed concrete, plastered or old painted surfaces after applying primer (exterior) |
| Unit | M2 |

| Definition | Acrylic based water-based paint on exposed concrete, plastered or old painted surfaces after applying primer (exterior) |
| --- | --- |

Pozu Recipe, Making Conditions

The price of 1 m², including all kinds of materials and supplies, labor, contractor's overheads and profit, necessary for the application of acrylic-based water-based paint of the desired color with an average of 0.222lt in 2 coats to the surface with a brush or roller, after removing the burrs and excessive grainy parts by scraping the surfaces to be painted, applying an average of 0.070lt primer in one coat, and applying acrylic-based water-based paint of the desired color to the surface with a brush or roller, 1 m² price

# SPECIAL POSITION 5: PAVING CONSTRUCTION

Making Jambs Making jambs with plate

| Definition | Making jambs with 3 cm thick 30cm x FREE SIZE plate ANDESITE PLAQUES (TS 10835) |
| --- | --- |
| Long Definition | MAKING JAMBS WITH 3 CM THICK PLATE |
| Unit | M2 |

Pose Description, Construction Conditions and Measurement

Thorough cleaning of the wall faces, wetting the wall face, making an average 3.5 cm thick, 400 kg dosed, cement dosed layer on the wetting of the wall face, making jambs with 3 cm thick plates to be monolithic, filling the corner joints with cement grout, replacing the broken and cracked plates during the coating, cleaning and wiping the coating face from mortar contaminants, all kinds of materials and wastes, including loading, horizontal and vertical transportation, unloading, labor, contractor's overhead and profit, 1 m2 price:

# SPECIAL POZ 6: PLASTIC JOINERY

| Pose No |  |
| --- | --- |
| Definition | Manufacturing and replacement of plastic joinery (all kinds of doors, windows, coatings and similar manufacturing from rigid pvc joinery profiles) |
| Long Definition | PLASTIC JOINERY MANUFACTURING AND REPLACEMENT (ALL KINDS OF DOORS, WINDOWS, COATINGS AND SIMILAR MANUFACTURING FROM HARD PVC JOINERY PROFILES) |

## Pose Description, Construction Conditions and Measurement

Plastic joinery and accessories and glazing beads made of rigid PVC profiles made according to the project and details must be resistant to all weather conditions and their surfaces must be smooth. The main profile made of PVC (wall thickness class "A" according to the standard and wall thickness on visible surfaces should be 2.8 mm and 2.5 mm on invisible surfaces) will have a pre-chamber system designed to accelerate both heat and sound insulation and also water drainage. Metal reinforcement profiles will provide the necessary strength of the main profiles (frame, sash, center register). Metal reinforcement profiles are U or box profiles made of sheet metal, protected against rust by hot dip galvanizing. In both cases, the sheet thickness shall not be more than 1.5 mm in the frame and wings and not more than 2 mm in the middle register. (However, if the moment of inertia is higher than the above-mentioned sheet thicknesses as a result of the calculation made in very wide registers and wings, sheet metal with a thickness compatible with the result should be used). Metal reinforced PVC profiles are combined with plastic corner welding, screws, wing binding and other means and all kinds of window joinery, doors, glass windows and similar manufacturing are made with the help of auxiliary joinery profiles, plates and other profiles. In accordance with the system proposed by the manufacturer, the wing gaps will be insulated with two rows of EPDM rubber, neoprene or tpe gaskets. The installation of glass of all types and thicknesses is done with the help of glazing beads. In accordance with the system recommended by the manufacturer, glass fixing shall be provided with gaskets, mastic and other methods. Each window sash frame (joinery) is fixed to the joinery frame with at least 2 (two) and door sash frame is fixed with at least 3 (three) hinges. The hinges shall be in strength and design to ensure the adjustable operation of the sash. The plastic joinery frame and wing compositions will be cut at 45 degrees and the plastic joinery manufactured by welding with machines developed for this work will be fixed to the masonry hitch or iron construction (blind frame). (Mounting to the masonry hitch can be in 3 ways. a) With clamp slats; Clamp slats are mounted to the joinery from one side with screws of suitable size, after the joinery is placed in place, the clamp slat is mounted to the masonry axle with screws of suitable size from the other side. b) With steel dowels; After the joinery is placed in place, a slot is opened with a drill so that it passes through the joinery to the masonry axle. In this slot, the steel dowel selected in the appropriate size is placed and tightened. c)With steel mounting screws; After the joinery is placed in place, a slot is opened with a drill so that it passes through the joinery to the masonry axle. In this slot, steel mounting screws selected in appropriate size are placed and tightened. Mounting to the blind frame can be done in 2 ways.

a) With sheet metal screws; After the joinery is placed in place, a slot is opened with a drill so that it also passes through the joinery to the blind frame. In this slot, sheet metal screws selected in the appropriate size are placed and tightened. b) With lock profiles; The first part of the lock profiles to be attached to the joinery is attached to the joinery from all sides. After the joinery is placed in place, the second part of the lock profiles is placed in place to lock with the first

part). All kinds of materials and waste, loading, horizontal and vertical transportation, unloading, labor, tools and equipment costs, contractor's overheads and profits, including contractor's overheads and profits, for ensuring impermeability to water, air and sound, and fixing the gaskets that will provide insulation in the wing gaps in accordance with the system, plastic joinery installed in place

# SPECIAL POSITION 7: DOUBLE GLAZED WINDOW UNIT

| Definition | Installing a double-glazed window unit with 4+4 mm thickness and 12 mm spacing with PVC and aluminum joinery profile and double-glazed window unit with heat control coating on the first glass |
| --- | --- |
| Long Definition | INSTALLATION OF DOUBLE-GLAZED WINDOW UNIT WITH 4+4 MM THICKNESS AND 12 MM SPACING WITH PVC AND ALUMINUM JOINERY WITH PROFILE AND DOUBLE-GLAZED WINDOW UNIT WITH FIRST GLASS HEAT CONTROL COATING |
| Unit | M2 |

Pose Description, Construction Conditions and Measurement

Preparation of 4+4 mm thick, 12 mm spaced, heat control coated, double glazed window unit according to the size of the place where it will be installed, placing wedges in the glass slot and placing the glass in the slot, fitting the profile and wick, balancing the unit with glazing wedges, The price of 1 m², including neutral (acid-free) silicone silicone in the form of punctuation at the joints of the profiles, loading, horizontal vertical transportation and unloading at the construction site, all kinds of materials and losses, labor, tools and equipment expenses, contractor overhead and profit: MEASURE: The areas where glass is installed are calculated according to the dimensions in the project. NOTE: Profile and wick cost is paid from its own joinery exposure.

| Special Pose No:8 | ATTIC INSULATION |
| --- | --- |
| Definition | Laying a 6 cm thick rock wool mattress (rock wool mattress - 50 kg/m3 density) on the slab between the roof and laying a waterproofing cover open to the passage of water vapor on it |
| Long Definition | LAYING A 6 CM THICK ROCK WOOL SLAB (ROCK WOOL SLAB - 50 KG/M3 DENSITY) ON THE SLAB BETWEEN THE ROOFS AND A WATERPROOFING COVER OPEN TO WATER VAPOR PASSAGE ON IT. |
| Unit | M2 |

Pose Description, Construction Conditions and Measurement

According to the project and details approved by the administration, laying 6 cm thick rock wool mattress on the slab between the roof without any gaps between them, fixing it to the purlins on the edge of the roof with slats when desired, laying the waterproofing cover open to water vapor passage on it so that it overlaps each other by at least 10 cm, The price of 1 m² including the laying of planks on wedges to provide access to the desired location between the roof, loading, horizontal and vertical transportation, unloading, all kinds of materials and losses, (excluding lath, wedge, plank and nail costs) labor, tools and equipment costs, contractor overhead and profit: MEASURE: All insulated surfaces are calculated according to the dimensions in the project. NOTE: The thickness of the rock wool mattress will be determined according to the heat calculation.